# CT  INT’L  ALUMINUM  CORP.

CT-50 Series 1-3/4” x 4-1/2”

Specifications

A. GENERAL DESCRIPTION

Work Included: Glazing Contractor to supply all necessary materials, labor and equipment for the complete installation of aluminum framing as shown on the drawings and specifications.

Work Not Included: Structural support of the framing system, interior closures, trim (please specify other exclusions).

B. QUALITY ASSURANCE

Drawing and specifications are based on C & T Series (CT-50/CT-51/CT-51T) centered glazed system. When required, supporting technical literature, samples, drawings and performance data will be submitted. Test reports certified by an independent test laboratory are to be made available upon request.

C. PERFORMANCE REQUIREMENTS

Air Infiltration shall be tested in accordance with ASTM E 283. Air infiltration shall not exceed .06 CFM per square foot (.0003m³/sm²) of fixed area when tested at 6.24 P.S.F. (300 Pa).

Water Infiltration shall be tested in accordance with ASTM E 331. No water penetration at test pressure of 8 P.S.F. (384 Pa).

Structural Performance shall be tested in accordance with ASTM E 330 and based on:

- Maximum deflection of  1/175  of the span

- Allowable stress with a safety factor of 1. 65

The system shall perform to this criteria under a windload of (please specify) P.S.F.

D. MATERIALS

Extrusions shall be 6063-T5 alloy and temper (ASTM B221 alloy T5 temper). Fasteners, where exposed, shall be aluminum, stainless steel or zinc plated steel in accordance with ASTM A 164. Perimeter anchors shall be aluminum or steel, providing the steel is properly isolated from the aluminum. Glazing gasket shall be E.P.D.M. elastomeric extrusions.

E. FINISH

All exposed framing surfaces shall be free of scratches and other serious blemishes. Aluminum extrusions shall be given a caustic etch followed by an anodic oxide treatment to obtain a Class I (7-mill. thick) standard (Please specify from below).

- Clear anodic coating   - Dark Bronze anodic coating   - Black anodic coating   -Other (specify finish)

A Fluoropolymer paint coating conforming with the requirements of the AAMA 605.2-92. Custom colors in a baked-on enamel or Duranar finish are also available.

F. FABRICATION

The framing system shall provide for flush glazing on all sides with no projecting stops. Vertical and horizontal framing members shall have a nominal face dimension of (please specify). Overall depth shall be (please specify). Entrance framing members shall be compatible with glass framing in appearance. Provide for internal drainage of infiltrated water into an extruded aluminum subsill channel where it is drained to the exterior of the system.

G. INSTALLATION

All glass framing shall be set in correct locations as shown in the details and shall be level, square, plumb and in alignment with other work in accordance with the manufacturer's installation instructions and approved shop drawings. All joints between framing and the building structure shall be sealed in order to secure a watertight installation.

H. PROTECTION AND CLEANING

After installation the General Contractor shall adequately protect exposed portions of aluminum surfaces from damage by grinding and polishing compounds, plaster, lime, acid, cement, or other contaminants, and all work by other trades. The General Contractor shall be responsible for final cleaning.