# CT  INT’L  ALUMINUM  CORP.

Series TD4800 Terrace Door

2 ⅛" Terrace Entrance Doors

Specifications

A. GENERAL DESCRIPTION

Work Included: Glazing Contractor to supply all necessary materials, labor and equipment for the complete installation of aluminum entrance doors frames, and hardware as shown on the drawings and specifications.

Work Not Included: Structural support of the framing system, interior closures, trim (specify other exclusions).

B. QUALITY ASSURANCE

Drawing and specifications are based on C & T TD4800 Series entrance doors.  When required, supporting technical literature, samples, drawings and performance data are to be submitted. Test reports certified by an independent test laboratory are to be made available upon request.

C. MATERIALS

Extrusions shall be 6063-T5 alloy and temper (ASTM B221 alloy T5 temper) unless otherwise specified.  The frame thermal barrier shall consist high density polyurethane.  The door leafs should be thermally isolated with two thermal struts mechanically crimped together. Fasteners, where exposed, shall be aluminum, stainless steel or zinc plated steel in accordance with ASTM A 164. Glazing gasket shall be E.P.D.M. elastomeric extrusions.

D. DOOR  AND FRAME CONSTRUCTION

Door leaf and frame shall consist of tubular aluminum members to be miter joined at comers with heavy concealed reinforcement anchors, hydraulically crimped. Door to have a snap-in stop with neoprene drive-in wedge against the exterior of glass.

E. HARDWARE

Hardware for aluminum doors and door frames are to be the entrance manufacturers standard. Three European profile hinges on each door are standard.  If custom hardware is to be furnished by others, templates and physical samples must be submitted prior to fabrication.

F. FINISH

All exposed framing surfaces shall be free of scratches and other serious blemishes. Aluminum extrusions shall be given a caustic etch followed by an anodic oxide treatment to obtain a (Please specify from below).

- Clear anodic coating (class 1 standard class 2 optional) - Dark Bronze anodic coating (class 1 standard) - Black anodic coating (class 1 standard) - Other (specify finish)

A Fluoropolymer paint coating conforming with the requirements of the AAMA 605.2-92. Custom colors in a baked-on enamel or Duranar finish are also available.

G. INSTALLATION

All items under this heading shall be set in correct locations as shown in the details and shall be level, square, plumb and in alignment with other work in accordance with the manufacturer's installation instructions and approved shop drawings. All joints between framing and the building structure are to be sealed to secure a watertight installation. Upon completion of the installation of the entrances, it shall be the contractor's responsibility to make all necessary final adjustments to attain normal operations of each door and its mechanical hardware.

H. PROTECTION AND CLEANING

After installation the General Contractor shall adequately protect exposed portions of aluminum surfaces from damage by grinding and polishing compounds, plaster, lime, acid, cement, or other contaminants, and all work by other trades. The General Contractor shall be responsible for final cleaning.